# PLA (Polylactic Acid)

## 1. What is PLA?

## Polylactic Acid (PLA), also known as polylactide, is a biodegradable thermoplastic polyester derived from renewable biological resources such as corn starch, sugarcane, or other carbohydrate-rich plants. PLA is produced from lactic acid monomers, which are typically obtained through fermentation of plant sugars. These monomers are then polymerized to form long polymer chains that create the PLA material.

Chemically, PLA is an aliphatic polyester composed of repeating units of lactic acid (2-hydroxypropanoic acid).

PLA is widely used in applications such as:

- 3D printing (FDM/FFF filaments)

- Food packaging

- biomedical implants

- disposable consumer products

Its popularity in additive manufacturing comes from its low melting temperature, minimal warping, and good layer adhesion.

References :- 
1. https://en.wikipedia.org/wiki/Polylactic_acid

2.https://www.sciencedirect.com/topics/agricultural-and-biological-sciences/polylactic-acid
3.sciencedirect.com

4.https://www.mdpi.com/2073-4360/13/8/1326

## 2. Properties of PLA

| SNO. | Property | Typical Value | Unit |
| --- | --- | --- | --- |
| 1 | Molecular Weight (Mw) | 66,000 | g/mol |
| 2 | Density | 1.21 – 1.27 | g/cm³ |
| 3 | Glass Transition Temperature (Tg) | 45 – 60 | °C |
| 4 | Melting Temperature (Tm) | 150 – 165 | °C |
| 5 | Tensile Strength | 21 – 60 | MPa |
| 6 | Yield Strength | 70 | MPa |
| 7 | Ultimate Tensile Strength | 73 | MPa |
| 8 | Young’s Modulus | 0.35 – 3.5 | GPa |
| 9 | Elastic Modulus | 3.5 | GPa |
| 10 | Shear Modulus | 1287 | MPa |
| 11 | Poisson’s Ratio | 0.36 | – |
| 12 | Elongation at Break | 2.5 – 7 | % |
| 13 | Ultimate Tensile Strain | 2.5 – 6 | % |
| 14 | Flexural Strength | 106 | MPa |
| 15 | Unnotched Izod Impact Strength | 195 | J/m |
| 16 | Notched Izod Impact Strength | 26 | J/m |
| 17 | Rockwell Hardness | 88 | HR |
| 18 | Heat Deflection Temperature | 55 | °C |
| 19 | Vicat Softening Temperature | 59 | °C |
| 20 | Specific Heat Capacity | 1590 – 2060 | J/kg·°C |
| 21 | Thermal Conductivity | 0.11 – 0.20 | W/m·°C |

References :- 
1. https://doi.org/10.1016/j.addr.2016.06.012
2. https://doi.org/10.1016/j.giant.2024.100261

## 3. Normal Process Parameters for PLA Printing

### 1. Nozzle Temperature 
Range : 180-220°C

### 2. Bed Temperature

| Range | Interpretation |
| --- | --- |
| 20–30 °C | No heated bed needed |
| 40–60 °C | Most common research setting |
| 60–70 °C | Improved adhesion |
| 70–100 °C | Still printable but less common |

Safe range : 40-70°C

### 3. Infill Density

Decorative Models: 10–20%

Medium Strength Parts: 40–60%

Functional Parts: 70–100%

### Print Speed

Range: 30–90 mm/s

References:-

1.10.1016/j.matpr.2019.09.078

2.10.3390/polym16131867

3.10.3390/polym13081239

4. Other Processing Methods For PLA

# 1. Melt Processing (Extrusion, Injection Molding)

Most PLA products are produced through melt processing, where PLA is heated above its melting temperature and shaped into a final part.

### Fabrication methods included

| Method | Description |
| --- | --- |
| Injection molding | Molten PLA injected into molds |
| Extrusion | PLA forced through die to make filaments or sheets |
| Film blowing | Thin PLA films for packaging |
| Thermoforming | Heating PLA sheets and shaping them |

These are very common industrial fabrication methods.

Reference :
1. https://doi.org/10.1016/j.progpolymsci.2008.05.004

# 2. Electrospinning (Nanofiber Fabrication)

In this study, PLA is dissolved in solvents and then electro spun into nanofibers using a high electric field.

### Application

- tissue engineering scaffolds

- biomedical materials

- filtration membranes

This is a completely different fabrication method from FDM.

Reference: 1.https://www.sciencedirect.com/org/science/article/pii/S1555256X21000825

3. Melt Blending and Composite Fabrication

This review describes several processing technologies used to fabricate PLA-based materials, including:

| Fabrication Method | Purpose |
| --- | --- |
| Melt blending | Mixing PLA with other polymers |
| Hot-melt extrusion | Producing PLA composites |
| Injection molding | Fabricating shaped parts |
| 3D printing | Additive manufacturing |

These methods are widely used to modify PLA properties.

Reference:

1.https://doi.org/10.1002/app.51839Digital Object Identifier (DOI)

4. Solvent Casting / Film Fabrication

In this method:

- PLA is dissolved in a solvent

- the solution is cast on a surface

- solvent evaporates forming a PLA film.

Applications include:

- food packaging

- biodegradable films

- medical coatings

Reference:

1.https://doi.org/10.1016/j.indcrop.2025.120460

5. Nanocomposite Fabrication Methods

The study explains different methods used to fabricate PLA nanocomposites:

| Method | Description |
| --- | --- |
| Melt mixing | blending nanoparticles into molten PLA |
| Sol-gel method | chemical synthesis of composites |
| In-situ polymerization | forming PLA composites during polymerization |

These methods are used to enhance

mechanical or thermal properties of PLA.

Reference:

1.10.3390/polym13183036

5. Orthotropic Properties of PLA Under Different Printing Parameters

| Sno | Authors | Title of the paper | Year | Printing Parameters Studied | Mechanical Tests Used | Key Findings | DOI/Paper link |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 1. | Shi Dai, Zi Chen Deng, Ya Jun Yu, Kai Zhang, Shu Heng Wang, Juan Ye | # Orthotropic elastic behaviors and yield strength of fused deposition modeling materials: Theory and experiments | 2020 | Printing direction, raster orientation | Tensile testing and SEM analysis | PLA printed by FDM shows strong orthotropic behavior. The C-plane (fiber–gravity plane) provides the highest stiffness and strength, while the B-plane shows the weakest performance. The orthotropic model predicts elastic modulus and yield strength more accurately than the transverse isotropic model. | https://www.sciencedirect.com/science/article/pii/S0142941819322238 |
| 2. | Gabriel Torrente-Prato, Luis Sosa-Vivas, Jhon Gonzalez-Delgado, Hernando Hernandez-Silva & Helia León-Molina | # Experimental and numerical study of the orthotropic behavior of 3D printed polylactic acid by material extrusion: part two: an analysis about poisson´s ratios | 2024 | Printing speed, Printing direction, | Uniaxial tensile test, Finite Element Method (FEM) simulation, Reverse engineering method | Poisson’s ratios in the plane perpendicular to the printing direction (νxy and νyx) are approximately equal and remain nearly constant regardless of printing speed or print direction when concentric fill patterns are used. Longitudinal specimens show higher density and mechanical strength than transverse specimens due to lower interlayer gaps and porosity. The study establishes a relationship between the density ratio of printed PLA and bulk PLA and the ratio of their Poisson’s ratios allowing estimation of Poisson’s ratios using density data. | https://link.springer.com/article/10.1007/s40964-024-00753-3 |
| 3. | Meiyu Li , Yanan Xu, Jianguang Fang | # Orthotropic mechanical properties of PLA materials fabricated by fused deposition modeling | 2024 | Raster angle, Air gap, Build orientation | Uniaxial tensile test,Digital Image Correlation, Digital Image Correlation | Interlayer bonding causes stronger anisotropy than intra-layer raster orientation, resulting in lower stiffness and tensile strength in the build (layer) direction. Introducing a −0.05 mm air gap significantly reduces internal voids, producing denser printed structures. The negative air gap improves elastic modulus and tensile strength compared with zero air gap samples. Despite improved bonding with a negative air gap, mechanical anisotropy remains due to oriented polymer chains and limited molecular diffusion between layers. | https://doi.org/10.1016/j.tws.2024.111800 |
| 4. | Luís Gonçalves, Gonçalo Couto, Armando Ramalho | The influence of layer height in the orthotropic elastic properties of PLA material obtained by additive processes | 2024 | Raster angle, Layer height | Impulse excitation of vibration (ASTM E1876-21 standard) | The study determined the orthotropic elastic constants E11, E22, E33, shear moduli G12, G23, and Poisson’s ratios ν12, ν23 using the impulse excitation vibration method (ASTM E1876-21). The transverse modulus E22 was consistently higher than the modulus in the filament deposition direction E11, confirming anisotropic stiffness in the deposition plane. Layer height affects the elastic properties because it influences porosity and filament bonding quality within the printed structure. Although elastic properties varied with layer height, no clear monotonic trend was observed, indicating that microstructural factors such as void formation and density variations significantly influence the mechanical response of printed PLA. | https://doi.org/10.1016/j.prostr.2024.01.012 |